###### SPTECH Silicon PNP Power Transistor         2SA1943

###### DESCRIPTION

·High Collector-Emitter Breakdown Voltage-

: V(BR)CEO= -230V(Min)

·Complement to Type 2SC5200

APPLICATIONS

·Power amplifier applications

·Recommended for 100W high fidelity audio frequency amplifier

output stage

### ABSOLUTE MAXIMUM RATINGS(Ta=25℃)

| SYMBOL | PARAMETER | VALUE | UNIT |
| --- | --- | --- | --- |
| VCBO | Collector-Base Voltage | -230 | V |
| VCEO | Collector-Emitter Voltage | -230 | V |
| VEBO | Emitter-Base Voltage | -5 | V |
| IC | Collector Current-Continuous | -15 | A |
| IB | Base Current-Continuous | -1.5 | A |
| PC | Collector Power Dissipation @ TC=25℃ | 150 | W |
| TJ | Junction Temperature | 150 | ℃ |
| Tstg | Storage Temperature Range | -55~150 | ℃ |

###### SPTECH Silicon PNP Power Transistor         2SA1943

ELECTRICAL CHARACTERISTICS

TC=25℃ unless otherwise specified

| SYMBOL | PARAMETER | CONDITIONS | MIN | TYP. | MAX | UNIT |
| --- | --- | --- | --- | --- | --- | --- |
| V(BR)CEO | Collector-Emitter Breakdown Voltage | IC= -50mA; IB= 0 | -230 |  |  | V |
| VCE(sat) | Collector-Emitter Saturation Voltage | IC= -8.0A; IB= -0.8A |  |  | -3.0 | V |
| VBE(on) | Base-Emitter On Voltage | IC= -7A; VCE= -5V |  |  | -1.5 | V |
| ICBO | Collector Cutoff Current | VCB= -230V; IE= 0 |  |  | -5 | μA |
| IEBO | Emitter Cutoff Current | VEB= -5V; IC= 0 |  |  | -5 | μA |
| hFE-1 | DC Current Gain | IC= -1A; VCE= -5V | 55 |  | 160 |  |
| hFE-2 | DC Current Gain | IC= -7A; VCE= -5V | 35 |  |  |  |
| COB | Output Capacitance | IE=0; VCB= -10V; f= 1.0MHz |  | 360 |  | pF |
| fT | Current-Gain—Bandwidth Product | IC=-1A ; VCE= -5V |  | 30 |  | MHz |

- hFE-1 Classifications

| R | O |
| --- | --- |
| 55-110 | 80-160 |