###### SPTECH Silicon NPN Darlington Power Transistor   2SD1071

###### DESCRIPTION

·Low Collector Saturation Voltage

·High DC Current Gain

·High Reliability

APPLICATIONS

·Audio power amplifiers

·Relay & solenoid drivers

·Motor controls

·General purpose power amplifiers

·Including zener diode

### ABSOLUTE MAXIMUM RATINGS(Ta=25℃)

| SYMBOL | PARAMETER | VALUE | UNIT |
| --- | --- | --- | --- |
| VCBO | Collector-Base Voltage | 450 | V |
| VCEO(SUS) | Collector-Emitter Voltage | 300 | V |
| VEBO | Emitter-Base Voltage | 6 | V |
| VZ | Zener Voltage | 300 | V |
| IC | Collector Current-Continuous | 6 | A |
| IB | Base Current-Continuous | 2.5 | A |
| PC | Collector Power Dissipation @ TC=25℃ | 40 | W |
| TJ | Junction Temperature | 150 | ℃ |
| Tstg | Storage Temperature Range | -40~150 | ℃ |

THERMAL CHARACTERISTICS

| SYMBOL | PARAMETER | MAX | UNIT |
| --- | --- | --- | --- |
| Rth j-c | Thermal Resistance,Junction to Case | 3.0 | ℃/W |

###### SPTECH Silicon NPN Darlington Power Transistor   2SD1071

ELECTRICAL CHARACTERISTICS

TC=25℃ unless otherwise specified

| SYMBOL | PARAMETER | CONDITIONS | MIN | TYP. | MAX | UNIT |
| --- | --- | --- | --- | --- | --- | --- |
| VZ | Zener Voltage | IZ= 0.1mA | 300 |  | 450 | V |
| V(BR)EBO | Emitter-Base Breakdown Voltage | IE= 5mA; IC= 0 | 6 |  |  | V |
| VCE(sat) | Collector-Emitter Saturation Voltage | IC= 4A; IB= 15mA |  |  | 1.5 | V |
| VBE(sat) | Base-Emitter Saturation Voltage | IC= 4A; IB= 15mA |  |  | 2.0 | V |
| ICBO | Collector Cutoff Current | VCB= 300V; IE= 0 |  |  | 0.1 | mA |
| IEBO | Emitter Cutoff Current | VEB= 6V; IC=0 |  |  | 5 | mA |
| hFE | DC Current Gain | IC= 4A; VCE= 2V | 500 |  |  |  |