###### SPTECH Silicon NPN Power Transistor          BU941T

###### DESCRIPTION

·High Voltage

·DARLINGTON

APPLICATIONS

·High ruggedness electronic ignitions

·High voltage ignition coil driver

### Absolute maximum ratings (Ta=25℃)

| SYMBOL | PARAMETER | VALUE | UNIT |
| --- | --- | --- | --- |
| VCBO | Collector-Base Voltage | 500 | V |
| VCEO | Collector-Emitter Voltage | 400 | V |
| VEBO | Emitter-Base Voltage | 5 | V |
| IC | Collector Current- Continuous | 15 | A |
| ICM | Collector Current-Peak | 30 | A |
| IB | Base Current | 1 | A |
| IBM | Base Current-Peak | 5 | A |
| PC | Collector Power Dissipation @TC=25℃ | 150 | W |
| Tj | Junction Temperature | 150 | ℃ |
| Tstg | Storage Temperature Range | -65~150 | ℃ |

THERMAL CHARACTERISTICS

| SYMBOL | PARAMETER | MAX | UNIT |
| --- | --- | --- | --- |
| Rth j-c | Thermal Resistance, Junction to Case | 1.2 | ℃/W |

###### SPTECH Silicon NPN Power Transistor          BU941T

ELECTRICAL CHARACTERISTICS

TC=25℃ unless otherwise specified

| SYMBOL | PARAMETER | CONDITIONS | MIN | TYP | MAX | UNIT |
| --- | --- | --- | --- | --- | --- | --- |
| VCEO(SUS) | Collector-Emitter Sustaining Voltage | IC= 50mA; IB= 0 | 400 |  |  | V |
| VCE(sat)-1 | Collector-Emitter Saturation Voltage | IC= 8 A; IB= 100mA |  |  | 1.6 | V |
| VCE(sat)-2 | Collector-Emitter Saturation Voltage | IC= 10 A; IB= 250mA |  |  | 1.8 | V |
| VCE(sat)-3 | Collector-Emitter Saturation Voltage | IC= 12 A; IB= 300mA |  |  | 2.0 | V |
| VBE(sat)-1 | Base-Emitter Saturation Voltage | IC= 8 A; IB= 100mA |  |  | 2.2 | V |
| VBE(sat)-2 | Base-Emitter Saturation Voltage | IC= 10 A; IB= 250mA |  |  | 2.5 | V |
| VBE(sat)-3 | Base-Emitter Saturation Voltage | IC= 12 A; IB= 300mA |  |  | 2.7 | V |
| ICES | Collector Cutoff Current | VCE= 500V;VBE= 0 VCE= 500V;VBE= 0;Tj=125℃ |  |  | 0.1 0.5 | mA |
| ICEO | Collector Cutoff Current | VCE= 450V;IB= 0 VCE= 450V;IB= 0;Tj= 125℃ |  |  | 0.1 0.5 | mA |
| IEBO | Emitter Cutoff Current | VEB= 5V; IC= 0 |  |  | 20 | mA |
| hFE | DC Current Gain | IC= 5A ; VCE= 10V | 300 |  |  |  |
| VECF | C-E Diode Forward Voltage | IF= 10A |  |  | 2.5 | V |