###### SPTECH Silicon PNP Darlington Power Transistor     MJ11015

###### DESCRIPTION

·Collector-Emitter Breakdown Voltage-

: V(BR)CEO= -120V(Min.)

·High DC Current Gain-

: hFE= 1000(Min.)@IC= -20A

·Low Collector Saturation Voltage-

: VCE (sat)= -3.0V(Max.)@ IC= -20A

·Complement to the NPN MJ11016

APPLICATIONS

·Designed for use as output devices in complementary

general purpose amplifier applications.

### Absolute maximum ratings (Ta=25℃)

| SYMBOL | PARAMETER | VALUE | UNIT |
| --- | --- | --- | --- |
| VCBO | Collector-Base Voltage | -120 | V |
| VCEO | Collector-Emitter Voltage | -120 | V |
| VEBO | Emitter-Base Voltage | -5 | V |
| IC | Collector Current-Continunous | -30 | A |
| IB | Base Current-Continunous | -1 | A |
| PC | Collector Power Dissipation @TC=25℃ | 200 | W |
| Tj | Junction Temperature | 200 | ℃ |
| Tstg | Storage Temperature Range | -55~+200 | ℃ |

THERMAL CHARACTERISTICS

| SYMBOL | PARAMETER | MAX | UNIT |
| --- | --- | --- | --- |
| Rth j-c | Thermal Resistance, Junction to Case | 0.87 | ℃/W |

###### SPTECH Silicon PNP Darlington Power Transistor     MJ11015

ELECTRICAL CHARACTERISTICS

TC=25℃ unless otherwise specified

| SYMBOL | PARAMETER | CONDITIONS | MIN | TYP. | MAX | UNIT |
| --- | --- | --- | --- | --- | --- | --- |
| V(BR)CEO | Collector-Emitter Breakdown Voltage | IC= -50mA; IB= 0 | -120 |  |  | V |
| VCE(sat)-1 | Collector-Emitter Saturation Voltage | IC= -20A; IB= -0.2A |  |  | -3.0 | V |
| V CE(sat)-2 | Collector-Emitter Saturation Voltage | IC= -30A; IB= -0.3A |  |  | -4.0 | V |
| VBE(sat)-1 | Base-Emitter Saturation Voltage | IC= -20A; IB= -0.2A |  |  | -3.5 | V |
| VBE(sat)-2 | Base-Emitter Saturation Voltage | IC= -30A; IB= -0.3A |  |  | -5.0 | V |
| ICBO | Collector Cutoff Current | VCB=-120V; IE=0 VCB=-120V; IE=0; TC=150℃ |  |  | -1.0 -5.0 | mA |
| ICEO | Collector Cutoff Current | VCE= -120V; IB= 0 |  |  | -1.0 | mA |
| IEBO | Emitter Cutoff Current | VEB= -5V; IC= 0 |  |  | -5.0 | mA |
| hFE-1 | DC Current Gain | IC= -20A, VCE= -5V | 1000 |  |  |  |
| hFE-2 | DC Current Gain | IC= -30A, VCE= -5V | 200 |  |  |  |