###### SPTECH Silicon NPN Power Transistor          2SD718

###### DESCRIPTION

·Collector-Emitter Breakdown Voltage-

: V(BR)CEO= 120V(Min)

·Good Linearity of hFE

·Complement to Type 2SB688

APPLICATIONS

·Audio frequency power amplifier applications

·Recommend for 45-50W audio frequency amplifier

output stage applications

### ABSOLUTE MAXIMUM RATINGS(Ta=25℃)

| SYMBOL | PARAMETER | VALUE | UNIT |
| --- | --- | --- | --- |
| VCBO | Collector-Base Voltage | 120 | V |
| VCEO | Collector-Emitter Voltage | 120 | V |
| VEBO | Emitter-Base Voltage | 5 | V |
| IC | Collector Current-Continuous | 8 | A |
| IB | Base Current-Continuous | 0.8 | A |
| PC | Collector Power Dissipation @ TC=25℃ | 80 | W |
| TJ | Junction Temperature | 150 | ℃ |
| Tstg | Storage Temperature Range | -55~150 | ℃ |

###### SPTECH Silicon NPN Power Transistor          2SD718

ELECTRICAL CHARACTERISTICS

TC=25℃ unless otherwise specified

| SYMBOL | PARAMETER | CONDITIONS | MIN | TYP. | MAX | UNIT |
| --- | --- | --- | --- | --- | --- | --- |
| V(BR)CEO | Collector-Emitter Breakdown Voltage | IC= 10mA ; IB= 0 | 120 |  |  | V |
| VCE(sat) | Collector-Emitter Saturation Voltage | IC= 5.0A; IB= 0.5A |  |  | 2.5 | V |
| VBE(on) | Base-Emitter On Voltage | IC= 5A ; VCE= 5V |  |  | 1.5 | V |
| ICBO | Collector Cutoff Current | VCB= 120V ; IE= 0 |  |  | 10 | μA |
| IEBO | Emitter Cutoff Current | VEB= 5V; IC= 0 |  |  | 10 | μA |
| hFE | DC Current Gain | IC= 1A ; VCE= 5V | 55 |  | 160 |  |
| COB | Output Capacitance | IE= 0; VCB= 10V;ftest= 1.0MHz |  | 170 |  | pF |
| fT | Current-Gain—Bandwidth Product | IC= 1A; VCE= 5V;ftest= 1.0MHz |  | 12 |  | MHz |

- hFE Classifications

| R | O |
| --- | --- |
| 55-110 | 80-160 |